SECTION 853	-	HOT MELT BITUMEN ADHESIVE FOR RAISED PAVEMENT MARKER INSTALLATION

853.01	DESCRIPTION

This section covers the requirements for hot melt bitumen adhesive for use in bonding raised pavement markers complying with the requirements of AS 1906 Part 3, to bituminous and concrete road surfaces.

The requirements relate to physical properties and packaging.

853.02	PHYSICAL PROPERTIES

Hot melt bitumen adhesive is a homogeneous mixture of bitumen and mineral filler.

#### Component Properties

(a)	Bitumen

Min.	Max.	Method

Penetration, 100 g, 5 s, 25(C	15	-	ASTM D5

Viscosity, 135(C, Poise	12	-	ASTM D2171

##### (b)	Filler

Min.	Max.

Filler content	% by dry mass of adhesive	65	75

Filler grading	% passing AS 0.150 mm sieve	100

% passing AS 0.075 mm sieve	85

#### Adhesive Properties	Min.	Max.	Method

Softening Point, (C	100	116	ASTM D36

Penetration	7	16	ASTM D5

Flow, mm	-	5	ASTM D3407 as modified

Heat Stability Flow, mm	-	5	ASTM D3407 as modified

Viscosity, 205(C, Poise	-	75	ASTM D2669 as modified

Flash Point, C.O.C., (C	250	-	ASTM D92

Shelf Life, years from date of delivery	2	-

Recommended Pouring Temperature, (C	185	220

#### Strength Requirements

Bond Strength Development

When tested in accordance with Appendix E of AS 3554 (as modified to allow use of hot melt adhesive), the adhesive shall attain a bond strength of 1.4 MPa within the times specified in Table 853.021.

Table 853.021  Maximum Times for Bond Strength Development

| (minutes) |
| --- |
| Adhesive | Bond Curing at 23(C | Bond Curing at 10(C | Bond Curing at 0(C |
| Bitumen Hot Melt | 35 | 35 | 35 |

Bond Strength in Slant Shear

When tested in accordance with Appendix F of AS 3554 (as modified to allow use of hot melt adhesive), the adhesive shall have minimum slant shear bond strengths as specified in Table 853.022.

Table 853.022  Slant Shear Failure Stress

| Substrate | Condition | Minimum Slant Shear Stress MPa |
| --- | --- | --- |
| Dry Steel | Adhesive bond cured for 24 ( 2 h at 23(C ( 2(C | 7 |
| Dry Steel | Adhesive bond cured for 24 ( 2 h at 23(C ( 2(C and water soaked for 7 days | 6.7 |
| Wet Hardened Concrete | Adhesive bond cured for 24 ( 2 h at 23(C ( 2(C | 5 |
| Wet Hardened Concrete | Adhesive bond cured for 24 ( 2 h at 23(C ( 2(C and water soaked for 24 h | 2.2 |
| Wet Hardened Concrete | Adhesive bond cured for 24 ( 2 h at 23(C ( 2(C and water soaked for 7 days | 3 |

Bond Strength in Shear

When tested in accordance with Appendix G of AS 3554 (as modified to allow use of hot melt adhesive), the adhesive shall have a minimum bond strength in compressive shear as specified in Table 853.023.

Table 853.023  Bond Strength in Shear

| Substrate | Minimum Bond Strength in Compressive Shear MPa |
| --- | --- |
| All ceramic and reflective markers in accordance with AS 1906.3, Types A, B and A/B, dry or bond cured for 24 ( 2 h at 23 ( 1(C and 7 days soak | 4.0 |

Bond Behaviour Under Impact Shear

When the adhesive is tested in accordance with Appendix H of AS 3554 (as modified to allow use of hot melt adhesive), there shall be no relative displacement of a slant shear block assembly when subjected to a drop impact energy of 150 J.

853.03	PACKAGING AND IDENTIFICATION

Each container shall display the following information:

- Manufacturer's Identification of Product

- Manufacturer's Name

- Supplier's Name

- Date of Manufacture

- Batch Number

- Directions for Using.

# Text boxes

Department of State Growth – August 2016

Section 853 (Page 1 of 2)

Department of State Growth – August 2016

Section 853 (Page 2 of 2)