SECTION 652	-	SUPPLY OF ELASTOMERIC BEARINGS

652.01	GENERAL

This section covers the manufacture and supply of laminated elastomeric bearings.

The manufacture and supply of elastomeric bearings shall be in accordance with AS 5100.4 Bridge design: Bearings and deck joints.

652.02	MATERIALS

Materials and components for use in bearings shall comply with AS 5100.4 Bridge design: Bearings and deck joints.

The completed bearings shall satisfy the structural performance and dimensional requirements of the design.

652.03	TOLERANCES

Dimensional tolerances for bearings shall be in accordance with AS 5100.4 Bridge design: Bearings and deck joints Appendix C.

652.04	BEARING TESTS

Bearings shall comply with the testing requirements of AS 5100.4 Bridge design: Bearings and deck joints and shall be tested in accordance with Appendix D.

All bearings shall be tested in compression and examined for splits, uneven bulging, delamination and other irregularity of shape.

Bearings that are split or which exhibit uneven bulging, delamination or other irregularity of shape shall be rejected.

Representative samples of bearings shall be subjected to shear stiffness testing.

Elastomeric bearings that do not meet shear stiffness testing criteria shall be rejected.

HP	Copies of all test certificates shall be provided to the Superintendent for review.

652.05	TRACEABILITY

Bearings shall be marked with a unique identification number and with the AS part number as listed in AS 5100.4 Bridge design: Bearings and deck joints Appendix A.

It shall be possible to identify bearings with the batch number of the elastomer and the associated test certificate number via the unique identification number.

Bearings shall be traceable from the point of manufacture to their final location via the unique identification number.

Copies of all traceability documents shall be provided to the Superintendent for review.

652.06	HANDLING, PACKING AND STORAGE

Elastomeric bearings shall be transported, stored and handled in a manner that prevents damage to the bearings.  Bearings that are damaged shall be rejected.

# Text boxes

Department of State Growth – August 2016

Section 652 (Page 1 of 1)